Tel 82-2-2675-5700  Fax82-22675-0576

mailto:tmc@tmc.co.kr

home-page;http://tmc.co.kr/

Cobalt Sulfate Monohydrate

Physical  properties

Formula              CoSO4.H2O

Molecular weight       172.93

Bulk density           0.5-0.7 g/cm3

Appearance           Pink powder, free flowing

Screen Size            95% min. thru. 30 mesh

##### Specification

lron(Fe+2)             33.0% min

Moisture              2.0% max

Lead,Pb               20 ppm max

Cadmium,Cd           10 ppm max

Arsenic, As             3 ppm max

Packing

25Kg, Kraft paper bag, Inner Polyethylene film