Tel 82-2-2675-5700 Fax 82-2- 2675-0576

mailto:tmc@tmc.co.kr

home-page;http://tmc.co.kr/

Analytical Report of Titanium Dioxide (Clinker)

Physical  properties

Formula              TiO2

Molecular weight       79. 9

Appearance           White Granular powder

Screen Size            9 mesh (2.00 mm)  100 % pass. ( 0 % residue max.)

20 mesh (0.85mm)   70 % pass. (30% residue max.)

65 mesh (0.21mm)   20 % pass. (80% residue max.)

100 mesh (0.15mm)  10 % pass. (90% residue max.)

##### Specification (lot no. )

|  | Unit | Guaranteed Analysis | Typical Anaylsis |
| --- | --- | --- | --- |
| TiO2 | % | 98.0 % min |  |
| SiO2 | % | 0.1 % max |  |
| Fe2O3 | % | 0.1% max |  |
| Sb2O3 | % | 0.2 % max |  |
| SO3 | % | 0.1 % max |  |
| H2O(moisture) | % | 0.20 max |  |
| Density | g/cm3 | 3.3~3.9 |  |
| Ignition Loss | % | 0.3 max |  |
| Matter soluble in Water | % | 0.6 max |  |
| pH |  | 7.0±0.5 |  |
| Any different materials |  | Not detected | none |
| The color |  | Not changed before/after | Standard this sample |

##### Package

1 Ton Jumbo bag / PP inner PE coating and PE liner(2 layer)

Each 2 big bags on the 1 pallet (1,100 cm X 1,000 cm X 10 cm )

in 20 ft container (20 MT)

Test and Inspector

----------------------------------------

Shim-yeon WHANG / manager

TMC Co.,Ltd  R&D Dept.