82-2-675-5700 fax 675-0576

mailto:tmc@tmc.co.kr

home-page;http://tmc.co.kr/

Copper Oxide

Physical  properties

Color                   Black to Brown finely divided powder

Bulk density             110-130 lbs./cu.ft.

Typical Sieve Analysis     99.8% thru No. 325 Mesh

Free-flowing, non-caking product

##### Specification

Copper oxide(CuO)        94.0% min

Copper as metallic         75.0% min

Lead,Pb                 50 ppm max

Arsenic,As               10 ppm max

Cadmium,Cd             20 ppm max

Packing

25Kg, Kraft paper bag, Inner polyethylene film