82-2-2663-2773 fax 2663-3372

tmc@tmc.co.kr   http://tmc.co.kr/

PVC (Poly Vinyl Chloride) Paste type

Physical  properties

Formula   :    [-CH2-CHCL-]n  M.W 30,000~100,000

Appearance :    white powder at normal temperature

HS code : 3903-90-00  (CAS No. 9002-86-2)

Solubility  :  Insoluble in Water, Petrolium, Alcohol, Chloro-hydrocarbon

##### Specification

| Index Name | CPM-31 | CPL-31 |
| --- | --- | --- |
| Average polymerizing Grade | 1.230 ~1,430 | 880 ~1,080 |
| Volatiles,% max. | 0.50 | 0.50 |
| Density,g/cm3 min.. | 0.2 ~ 0.4 | 0.2 ~ 0.4 |
| Sieve residue, ppm, max | 10 | 10 |
| B type Viscosity (V6) | 500~2,500 | 1,500 ~ 6,500 |
| use | leather, shoes, toy plastics | wall paper, paper coating. |

Packing

20Kg, Plastic lined PP woven bag

500kg Jumbo bag, on pallet.  19.5 Mt/40ft’ container