82-2-2663-2773 fax 2663-3372

tmc@tmc.co.kr   http://tmc.co.kr/

PVC (Poly Vinyl Chloride) Strait type

Physical  properties

Formula   :    [-CH2-CHCL-]n  M.W 30,000~100,000

Appearance :    white powder at normal temperature

HS code : 3903-90-00  (CAS No. 9002-86-2)

Solubility  :  Insoluble in Water, Petrolium, Alcohol, Chloro-hydrocarbon

##### Specification

| Index Name | TMC-SG5 | TMC-SG7 |
| --- | --- | --- |
| Viscosity ml/g(K value){P } | 118-107(68-65) {1100-1000} | 95-87(62-60) {850-750} |
| Volatiles,% max. | 0.40 | 0.40 |
| Spots max. | 30 | 40 |
| Density,g/ml min.. | 0.42 | 0.45 |
| 0.25um mesh max. | 2.0 | 2.0 |
| "Fish Eyes"/400 cm2 max. | 40 | 50 |
| Abs.of plas.by 100PVC, g min. | 19 | 14 |
| Whiteness (160degree,10min) % min | 74 | 70 |
| Extr. Cond. S/m max. | 5X10-3 | 5X10-3 |
| Res. of CE PPM max. | 10 | 10 |
| GB4803-84 Stand food grade PVC, Res. of CE PPM max. | 5 | 5 |
| use | Window frame,Pipe strait | Sheet, film paste |

Packing

25Kg, Plastic lined PP woven bag

1 MT Jumbo bag, on pallet