82-2-2663-2773 fax 2663-3372

tmc@tmc.co.kr     http://tmc.co.kr/

Zinc Oxide 99.5% Granular

Physical  properties

Formula                 ZnO

Appearance              White powder (slightly yellow)

Screen Size              20 mesh ~ 80 mesh (0.5~1.5 mm)

Solubility                Insoluble in Water

##### Specification

ZnO                    99.5% min Granular

PbO                    0.12% max

CdO                    0.02% max

CuO                    0.006% max

Metallic Zinc             none

Mn                     0.0002% max

Insoluble HCI            0.02% max

Loss in ignition           0.4% max

Packing

20Kg, Kraft paper bag, Inner Polyethylene film, 1 MT Jumbo bag

Qty/Fcl : 20 Mt = 1 Fcl