82-2-2663-2773 fax 2663-3372

tmc@tmc.co.kr     http://tmc.co.kr/

Zinc Oxide 99.5% Powder

Physical  properties

Formula                 ZnO

Appearance              White powder (slightly yellow)

Screen Size              99.65 % min. thru. 325 mesh

Solubility                Insoluble in Water

##### Specification

ZnO                   99.5% min POWDER

PbO                   0.12% max

CdO                   0.02% max

CuO                   0.006% max

Metallic Zinc            none

Mn                    0.0002% max

Insoluble HCI            0.02% max

Loss in ignition           0.4% max

Packing

20Kg, Kraft paper bag, Inner Polyethylene film, 1 MT Jumbo bag

Qty/Fcl : 20 Mt = 1 Fcl