82-2-2663-2773 fax 2663-3372

tmc@tmc.co.kr     http://tmc.co.kr/

Zinc Oxide 99% Powder

Physical  properties

Formula                	ZnO

Appearance             	White powder (slightly yellow)

Screen Size              99.65 % min. thru. 325 mesh

Solubility                Insoluble in Water

##### Specification

ZnO                   	99.0 % min POWDER

PbO                   	0.2 % max

CdO                   	0.05% max

CuO                   	0.008% max

Metallic Zinc            none

Mn                    	0.0003% max

Insoluble HCI           	0.03% max

Loss in ignition          	0.6% max

Water soluble            0.7% max

Water contents          		0.2% max

Packing

20Kg, Kraft paper bag, Inner Polyethylene film, 1 MT Jumbo bag

Qty/Fcl : 20 Mt = 1 Fcl  Two Big bag on 1 pallet