Tel 82-2-2675-5700  Fax 82-2- 2675-0576

mailto:tmc@tmc.co.kr www.http://tmc.co.kr/

Technical Bulletin (Titanium Dioxide)

Titanium Dioxide Preparation : TMC-A100

Our TMC- A100 is widely used in white color Industry, such

as paint, paper making, wall paper making, Master bath, Ink

Ceramic, Tire, Road marker, Rubber thread, PVC & Vinyl !

We produce 1,500 MT/month of TMC-A100 for South-east

Asia area. TMC-A100 is guaranteed by below specification.

Physical  properties

Formula              TiO2

Molecular weight       79. 9

Appearance           White Powder

Screen Size           325 mesh. 99.90% pass

##### Specification

| Component | Unit | Guaranteed Analysis |
| --- | --- | --- |
| TiO2 | % | 90~95 % min |
| H2O | % | 0.3 % max |
| Residue(325mesh) | % | 0.1 %max |
| Oil Absorption | cc/100g | 26 max |
| Lightening Power | % | 105 |
| Matter soluble in Water | % | 0.6 max |
| pH |  | 7.0~7.4 |
| Dispersion rate( in water) | % | 70.0 % min |
| Whiteness enforcement agent |  | 3~8 % |

Packing

25kg  Paper bag, or  500 kg / 1 MT  Jumbo bag.