The Test result data of PVC Resin  (strait type : TMC SG-5)

In WINDOW FRAME making

- Data Base of PVC : TMC SG-5

| Items | Unit | standard | Result data |
| --- | --- | --- | --- |
|  |  |  | Control(P-1000) | TMC SG-5 |
| Flow | sec | 20 max. | 12.80 | 21.75 |
| Bulk density | g/cc | 0.55 min. | 0.651 | 0.631 |
| particle(250 ㎛) | % | 95% pass | 98.16 | 99.03 |
| Impurities no. | ea/100g | 10 max. | 0 | 0 |
| Water contents | % | 0.3 max. | 0.15 | 0.16 |
| Color difference | ΔE | 3.0 max. | 2.06 | 2.02 |
|  |  | L | 95.8 | 95.83 |
|  |  | a | -0.23 | -0.11 |
|  |  | b | 0.73 | 0.95 |

- Control ( HANWHA PVC resin (P-1000)

- Test SAMPLE ( TMC SG-5

- the DATA of Extrusion Process

|  | Result DATA on several Extruder |
| --- | --- |
|  | Large sized E. | Middle sized E. | High speed E. |
| Cylinder part (‘C) | C1 | 185 | 185 | 170 | 169 | 179 | 180 |
|  | C2 | 188 | 188 | 178 | 177 | 190 | 190 |
|  | C3 | 185 | 1185 | 175 | 175 | 189 | 190 |
|  | C4 | 180 | 180 | 168 | 168 | 185 | 185 |
|  | C5 | 167 | 167 | - | - | 174 | 175 |
|  | C6 | - | - | - | - | 170 | 170 |
| ADAP’TEMP(‘C) | 170 | 170 | 170 | 170 | 172 | 172 |
| SCREW TEMP(‘C) | 145 | 145 | 144 | 145 | - | - |
| RESIN TEMP(‘C) | 196 | 196 | 196 | 197 | 196 | 196 |
| DIES(‘C) | D1 | 195 | 195 | 195 | 195 | 198 | 198 |
|  | D2 | 195 | 196 | 197 | 197 | 195 | 195 |
|  | D3 | 195 | 195 | 195 | 195 | 190 | 190 |
|  | D4 | 193 | 194 | 193 | 193 | 195 | 195 |
| MELT Pressure(bar) | 204-205 | 214-218 | 191 | 201 | 246-247 | 253- 254 |
| Raw material Feed RPM | 23.0 | 23.0 | 98.0 | 98.0 | 23.6 | 21.5 |
| SCREW RPM | 15.0 | 15.0 | 24.2 | 24.2 | 16.1 | 16.1 |
| Extrusion LOAD(%) | 51-52 | 52-53-54 | 62-63 | 59-60 | 41-42 | 38-39 |
| Speed (M/min) | 2.68 | 2.68 | 1.62 | 1.55 | 1.89 | 1.80 |

※ Large sized Extruder  :  180Kg/hr  Paraller   Screw

※ Middle sized Extruder  :  100Kg/hr  Conical   Screw

※ High speed Extruder :  350Kg/hr  Paraller   Screw

- Quality test DATA of Products

| Test | Unit | Standard | Result |
| --- | --- | --- | --- |
|  |  |  | Control | TMC SG-5 |
| Appearance | - | Smooth and without air bubble | good | good |
| Sizing | mm | Size As same as standard demand | good | good |
| Assembleing | - | Easy and tight assemble as drawing | good | good |
| Bending | mm | 1mm max. at 1,000 mm center | good | good |
| Glossness | - | 20 min. | 41,9 | 29.3 |
| weight | g/m | 1,230±62 | 1,182 | 1,170 |
| Color difference | ΔE | 1.3 max. | 0.94 | 0.85 |
|  |  | L | 94.00 | 93.99 |
|  |  | a | -0.60 | -061 |
|  |  | b | 0.79 | 0.88 |

- Physical properties of Products.

| items | Unit | Standard | Result Data |
| --- | --- | --- | --- |
|  |  |  | Control | TMC SG-5 |
| hardness | ㅡ | 85 min. | 103 | 104 |
| Tensile strength | MN/㎡ | 36.8 min. | 38.41 | 39.1 |
| Elongation (Break) | % | 100 min | 169.2 | 167.3 |
| Flexural Modulus | MN/㎡ | 1961 min | 2499 | 2493 |
| Low temp. Impact | ㅡ | not more than 2 Crack | no | no |
| Heat Deflection | ㅡ | no blowhole,crack,feeling-off | no | no |
| Burning-Resistant | ㅡ | Not burning | no | no |
| Sharpy Impact(23’C) | KJ/㎡ | 12.7 min. | 68.3 | 81.9 |
| Sharpy Imp. (-10’C) | KJ/㎡ | 4.9 max. | 20.2 | 23.2 |
| Heat elongation | % | 2.5 min. | 1.61 | 1.58 |
| Low temp. shrinkage | % | 0.2 min. | 0.10 | 0.06 |

- the Test of Heat Stability

| Min ( ΔE) | 0 | 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Control | 0 | 0.97 | 1.59 | 2.8 | 4.44 | 5.83 | 7.28 | 8.62 | 9.99 | 10.91 | 11.19 |
| TMC SG-5 | 0 | 0.81 | 1.79 | 3.13 | 4.81 | 6.42 | 7.69 | 8.82 | 9.57 | 10.13 | 10.8 |

- The Physical properties of WINDOW FRAME ( WELDING STRENGTH)

| Test No | Unit | Standard | Result data |
| --- | --- | --- | --- |
|  |  |  | Control | TMC SG-5 |
| Welding Strength | NO 1 | N | 1,500 min. | 4253.2 | 4664.8 |
|  | NO 2 |  |  | 4027.8 | 3900.4 |
|  | NO 3 |  |  | 3645.6 | 3537.8 |
|  | NO 4 |  |  | 4390.4 | 5184.2 |
|  | NO 5 |  |  | 4370.8 | 3969.0 |
| Average | 4137.6 | 4251.2 |

| Process Moniter | Product size | result | Process Moniter | Product size | result |
| --- | --- | --- | --- | --- | --- |
| Cylinder | C1 | 185 | 1 | 65.0±0.5 | 64.71 | ScrewTemp | 145 | 12 | 3.0±0.5 | 3.05 |
|  | C2 | 188 | 2 | 48.0±0.5 | 48.50 | Resin Temp | 196 | 13 | 11.9±0.5 | 11.95 |
|  | C3 | 185 | 3 | 36.5±0.5 | 36.71 | Screw RPM | 15.0 | 14 | 2.2±0.5 | 2.21 |
|  | C4 | 180 | 4 | 16.0±0.5 | 15.89 | % | 53.0 | (t) | 2.0±0.5 | 2.15 |
|  | C5 | 167 | 5 | 4.5±0.5 | 4.71 | Feed RPM | 23.0 | Melt presure | 214 |
|  | C6 |  | 6 | 4.5±0.5 | 4.73 | Ext.vacuum | 110 | result | Passed |
|  | A1 | 170 | 7 | 2.8±0.5 | 2.74 |  |
| Dies | D1 | 194 | 8 | 2.8±0.5 | 2.75 |  |
|  | D2 | 195 | 9 | 7.3±0.5 | 7.03 |  |
|  | D3 | 195 | 10 | 7.3±0.5 | 7.09 |  |
|  | D4 | 193 | 11 | 8.0±0.5 | 8.11 |  |
| Cal 1 | 0.89 | Cal 2 | 0.72 | Cal 3 | - | Cal 4 | 0.23 |
| Speed | 2.68 | Process | 14 |  | - |
| Test Item | Standard | Test result | pass |
| weight | g/m | 780 ± 39 | 761.58 | Pass |
| bending | mm | 1mm max. at 1,000 mm center | good | Pass |
| glossness | - | 20 min | 41.1 | Pass |
| elongation | % | 2.5 max | 1.89 1.9 1.92 1.90 | Pass |
| Color difference | △E | 1.3 max | 0.24 | Pass |
|  |  | L a b | 93.86 -0.54 1.61 |  |
| Appreance | Crack, undulation | Good forming and smooth surface | good | Pass |
|  | Sink mark, carbonize |  | good |  |
|  | Weld line, break |  | good |  |
|  | impurites, air bubble |  | good |  |
|  | Mal-forming |  | good |  |
| Assembleing | IL-0930,GB-093N RS-0900/1 GASKET, MOHAIR |  | Tightly fit and easy assemble | good | Pass |

- Final result DATA sheets of Products (on several types of Extruder)

7-1 Large-sized Extruder (180Kg/hr  Paraller Screw)

7-2 Middle-sized Extruder (100Kg/hr  Conical Screw)

| Process Moniter | Product size | result | Process Moniter | Product size | result |
| --- | --- | --- | --- | --- | --- |
| Cylinder | C1 | 170 | 1 | 80.0±0.5 | 80.02 | ScrewTemp | 145 | 12 | 3.0±0.3 | 2.99 |
|  | C2 | 178 | 2 | 61.0±0.5 | 61.12 | Resin Temp | 197 | 13 | 14.5±0.5 | 14.82 |
|  | C3 | 175 | 3 | 41.5±0.5 | 41.65 | Screw RPM | 24.2 | 14 | 2.2±0.5 | 2.15 |
|  | C4 | 168 | 4 | 16.0±0.5 | 15.96 | % | 59.0 | (t) | 2.8±0.2 | 2.81 |
|  | C5 | - | 5 | 4.5±0.5 | 4.35 | Feed RPM | 98 | Melt Pressure | 201 |
|  | C6 |  | 6 | 4.5±0.5 | 4.37 | Ext.vacuum | 160 | Result | Passed |
| Dies | A1 | 170 | 7 | 2.8±0.5 | 3.05 |  |
|  | D1 | 195 | 8 | 2.8±0.5 | 3.09 |  |
|  | D2 | 197 | 9 | 7.1±0.5 | 7.12 |  |
|  | D3 | 195 | 10 | 7.1±0.5 | 7.16 |  |
|  | D4 | 193 | 11 | 8.0±0.5 | 8.09 |  |
| Cal 1 | 0.89 | Cal 2 | 0.60 | Cal 3 | - | Cal 4 | 0.30 |
| Speed | 1.55 | process | 12 |  | - |
| Test item | standard | Test result | Pass |
| weight | g/m | 1,230±62 | 1,170.00 | Pass |
| bending | mm | 1mm max. at 1,000 mm center | good | Pass |
| glossness | - | 20 min | 29.3 | Pass |
| elongation | % | 2.5 max | 1.60 1.58 1.56 1.58 | Pass |
| Color difference | △E | 1.3 max | 0.85 | Pass |
|  |  | L a b | 93.99 -0.61 1.88 |  |
| Appreance | Crack, undulation | Good forming and smooth surface | good | Pass |
|  | Sink mark, carbonize |  | good |  |
|  | Weld line, break |  | good |  |
|  | impurites, air bubble |  | good |  |
|  | Mal-forming |  | good |  |
| Assembleing | IL-0700,GB-042N RS-0700/1 |  | Tightly fit and easy assemble | good | Pass |

7-3 High-speed Extruder (350Kg/hr  Paraller Screw)

| Process Moniter | Product size | result | Process Moniter | Product size | result |
| --- | --- | --- | --- | --- | --- |
| Cylinder | C1 | 180 | 1 | 224.±0.5 | 224.18 | ScrewTemp | - | 12 | 12.0±0.5 | 12.14 |
|  | C2 | 190 | 2 | 53.0±0.5 | 53.21 | Resin Temp | 179 | 13 | 12.0±0.5 | 12.21 |
|  | C3 | 190 | 3 | 49.0±0.5 | 48.99 | Screw RPM | 16.1 | 14 | 12.0±0.5 | 12.22 |
|  | C4 | 185 | 4 | 49.0±0.5 | 48.93 | % | 38.2 | 15 | 8.0±0.5 | 2.81 |
|  | C5 | 175 | 5 | 16.7±0.5 | 16.68 | Feed RPM | 21.5 | (t) | 2.4±0.2 | 2.31 |
|  | C6 | 170 | 6 | 34.5±0.5 | 34.54 | 압출진공 | 150 | Melt 압력 | 254 |
| Dies | A1 | 172 | 7 | 52.0±0.5 | 52.07 |  |
|  | D1 | 198 | 8 | 34.5±0.5 | 34.33 |  |
|  | D2 | 195 | 9 | 24.8±0.5 | 24.68 |  |
|  | D3 | 190 | 10 | 5.5±0.5 | 5.57 |  |
|  | D4 | 195 | 11 | 12.0±0.5 | 12.12 |  |
| Cal 1 | 0.75 | Cal 2 | 0.54 | Cal 3 | - | Cal 4 | 0.27 |
| speed | 1.80 | process | 15 |  | - |
| Test item | standard | Test result | Pass |
| weight | g/m | 2,746±62 | 2,630.00 | Pass |
| bending | mm | 1mm max. at 1,000 mm center | good | Pass |
| glossness | - | 20 min | 29.3 | Pass |
| elongation | % | 2.5 max | 1.35 1.38 1.37 1.37 | Pass |
| Color difference | △E | 1.3 max | 0.67 | Pass |
|  |  | L a b | 93.91 -0.61 1.07 |  |
| Appreance | Crack, undulation | Good forming and smooth surface | good | Pass |
|  | Sink mark, carbonize |  | good |  |
|  | Weld line, break |  | good |  |
|  | impurites, air bubble |  | good |  |
|  | Mal-forming |  | good |  |
| Assembleing | IL-0700,GB-042N RS-0700/1 |  | Tightly fit and easy assemble | good | pass |

- Appedix  : detail data of physical properties (TMC PVC SG-5)

8-1-1 Sharpy Impact Strength ( std. temp.23’C)

| No. | Width | Thickness | Absorbed Energy | Resilience | Broken | read |
| --- | --- | --- | --- | --- | --- | --- |
|  | ① mm | ② mm | ③ J | ④ KJ/㎡ | ⑤ Kgf ㎝/㎠ |  |  |
| 1 | 9.75 | 2.52 | 2.176 | 87.9 |  |  | 81.9 |
| 2 | 9.75 | 2.52 | 1.908 | 77.0 |  |  |  |
| 3 | 9.75 | 2.52 | 1.986 | 80.2 |  |  |  |
| 4 | 9.75 | 2.52 | 1.932 | 78.0 |  |  |  |
| 5 | 9.75 | 2.52 | 2.134 | 86.2 |  |  |  |

8-1-2 Sharpy Impact Strength (low temp. -10’C)

| No. | Width | Thickness | Absorbed Energy | Resilience | Broken | read |
| --- | --- | --- | --- | --- | --- | --- |
|  | ① mm | ② mm | ③ J | ④KJ/㎡ | ⑤Kgf ㎝/㎠ |  |  |
| 1 | 9.75 | 2.52 | 0.616 | 24.4 |  | ● | 23.6 |
| 2 | 9.75 | 2.35 | 0.544 | 23.0 |  | ● |  |
| 3 | 9.75 | 2.52 | 0.536 | 21.2 |  | ● |  |
| 4 | 9.75 | 2.52 | 0.568 | 22.5 |  | ● |  |
| 5 | 9.75 | 2.52 | 0.672 | 26.7 |  | ● |  |

Calculation  (Sharpy Impact strength))

③ W a cN ④ = ----- x 10 3 = ------ x 10 3 ① x ② h bN

W ③ : Absorbed Impact Energy (J) h ② : width of sample with notch(㎜) bN ① : Thickness of sample with notch(㎜) Impact strength of sharpy : 4J

8-2 Tensile , Yield Point and  Elongation(break) (std. temp.23’C)

| No. | Width | Thickness | Yield | Tensile | length | ⑥ | Elongation (%) |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | ① mm | ② mm | ③ Kgf ㎝/㎠ | ④after (mm) | ⑤before (mm) |  |  |
| 1 | 5.75 | 2.52 | 3.954 |  | 25 | 60.92 | 1.680 | 168.0 |
| 2 | 5.75 | 2.52 | 4.102 |  | 25 | 63.11 | 1.777 | 177.7 |
| 3 | 5.75 | 2.52 | 3.873 |  | 25 | 62.95 | 1.770 | 177.0 |
| 4 | 5.75 | 2.52 | 4.068 |  | 25 | 60.15 | 1.647 | 164.7 |
| 5 | 5.75 | 2.52 | 3.960 |  | 25 | 56.61 | 1.491 | 149.1 |
| Avg. | 5.75 | 2.52 | 3.991 |  | 25 | 60.73 | 1.673 | 167.3 |

Elongation (break) =  ⑥ x 100 = { (⑤ x 1.1 - ④ ) / ④ } x 100

8-3 Flexural Modulus

| No. | Length of Test point | Length of sample | Height of sample | weight | bias | Elongation (break) |
| --- | --- | --- | --- | --- | --- | --- |
|  | L | B | H | F | Y | Ef |
| 1 | 40 | 24.75 | 2.52 | 12.65 | 2.0 | 255.6 |
| 2 | 40 | 24.75 | 2.52 | 12.62 | 2.0 | 254.9 |
| 3 | 40 | 24.75 | 2.52 | 12.51 | 2.0 | 252.7 |
| 4 | 40 | 24.75 | 2.52 | 12.57 | 2.0 | 253.9 |
| 5 | 40 | 24.75 | 2.52 | 12.60 | 2.0 | 254.5 |
| 평균 | 40 | 24.75 | 2.52 | 12.59 | 2.0 | 254.3 |

Flexural Modulus   Ef = L³ ÷ 4BH³ × F ÷ Y

|  | ☞ Ef*9.8=MN/㎡ |
| --- | --- |

8-4 Burn-resistance test

|  | No. of sample | Avg. |
| --- | --- | --- |
|  | 1 | 2 | 3 | 4 | 5 |  |
| time(sec) | 0 | 0 | 0 | 0 | 0 | 0 |
| length(mm) | 10.96 | 11.03 | 11.12 | 11.18 | 11.24 | 11.11 |
| types | Non flammable | o | o | o | o | o | Non Flammable |
|  | Self extinguish |  |  |  |  |  |  |
|  | flammable |  |  |  |  |  |  |

8-5 Elongation/shrinkage test on temperature change(reapeat)

|  | No. of sample | Avg. |
| --- | --- | --- |
|  | 1 | 2 | 3 | 4 | 5 |  |
| length (mm) | before | 450.00 | 450.00 | 450.00 |  |  | 450.00 |
|  | after | 449.74 | 449.68 | 449.76 |  |  | 449.73 |
| Result (%) | 0.06 | 0.07 | 0.05 |  |  | 0.06 |

8-6 the strength against Falling ball at low temp.

|  | No. of sample | total |
| --- | --- | --- |
|  | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 |  |
| N / B | ●/ | ●/ | ●/ | ●/ | ●/ | ●/ | ●/ | ●/ | ●/ | ●/ | 10/0 |

8-7 Hardness, Heat distortion

| item | unit | No. of sample | Avg. |
| --- | --- | --- | --- |
|  |  | 1 | 2 | 3 | 4 | 5 |  |
| hardness | ㅡ | 104.5 | 103.8 | 104.3 | 104.1 | 104.2 | 104.2 |
| Heat distortion | ㅡ | Not detected | Not detected | Not detected | Not detected | Not detected | Not detected |

8-8 The Strength test after welding

| Before welding | After welding |
| --- | --- |