Test result of Calcite (CaCO3 CA-400, CA-800)

2006.8.7

1.  Sample

Control(Korean products) / CA-400, CA-800, CA-1250 / Taiwan products

2. Purse of test

As filler properties in Wall paper

3. Test Method

Chemical, Physical properties : Wall paper standard test method.

Whiteness :Minolta CM508i,

Oil asorption : mixing with DOP

Particles size difference :  Mastersizer X.

Particle shape : SEM (Electro microscope)

4. Test Result

1) Chemical / Physical properties

| Items | Unit | Test result |
| --- | --- | --- |
|  |  | control | CA1250 | CA-800 | CA400 | Taiwan |
| Whiteness | L | 97.46 | 98.88 | 98.84 | 98.71 | 97.95 |
|  | a | -0.01 | -0.10 | -0.04 | -0.03 | -0.07 |
|  | b | -0.13 | 0.73 | 0.76 | 0.87 | 0.35 |
| Particle | d(0.5) | 5.97 | 3.32 | 5,90 | 10.32 | 3.41 |
|  | D(4,3) | 9.63 | 3.89 | 9.99 | 13.60 | 7.34 |
|  | d(0.9) | 15.50 | 7.65 | 14.32 | 29.41 | 19.42 |
| Oil Absorption | mL/100g | 37.3 | 30.0 | 30 | 26.7 | 27.6 |
| Color change After oil absorption | L | 90.54 | 94.41 | 94,41 | 94.27 | 89.65 |
|  | a | -0.42 | -0.44 | -0.40 | -0.20 | -0.41 |
|  | b | 0.43 | 5.47 | 0.41 | 4.57 | 2.67 |

2) Particle size analysis

3) particle shape (SEM)

4) Sample apply test in wall paper

| Sample Name | Result |
| --- | --- |
|  | L | a | b |
| CA-400 | 88.80 | -0.95 | 4.65 |
| Taiwan | 86.70 | -1.00 | 5.82 |
| Control1 | 81.52 | -0.93 | 9.85 |
| Control2 | 77.51 | 0.89 | 13.37 |

5. Conclusion

TMC CA-400 and CA-800 have a good properties in general test of wall paper making process. we could easy control color harmonization and color formation because the Whiteness is better than other filler(Korean product and Taiwan product), we concluded  to reduce using not only white supplements  but also Plsticiser(DOP).

| Calcite | 0.1kg | 1kg | 1000kg | 100,000kg |
| --- | --- | --- | --- | --- |
| DOP reduced | 0.9g | 9g | 9kg | 900kg |

# Text boxes

CA-400

Taiwan

Cont 1

Cont 2

Cont 2

Cont 1

ContControl1

Taiwan

CA-400