Viscosity test

- Purpose

To define the method to determine the Viscosity of Raw material dispersion

- Equipment

  - Brookfield viscometer LVT

  - Cooling bath

- Reagent

N/A

- Documentation

  - Raw material analysis record book (DF 6.10)

  - Dispersion analysis record book (DF 6.04)

- Procedure

  - Stir homogeneously the raw material dispersion with a manual stirrer and

Fill it very carefully to the brim of 400 ml tall from beaker to avoid bubble

formation. Remove the bubble with paper.

  - adjust the raw material dispersion to 30 ± 1 ‘C and simultaneously stir to get uniform temperature.

  - Check the viscosity with Brookfield viscometer spindle 4, speed 30 and speed 60.

  - Now down reading when it stabilized.

- Result

Viscosity of raw material dispersion =

Reading for speed 30 x 40 at 30’C - Reading for speed 60 x 20 at 30’C

PT swasthi   parama mulya. Cibitung compound department

Dispersion TiO2 65 % (DT)

Titanium dioxide 2000.00

Darvan No. 7        4.52    vande-l? : high solid dispersion agent

DMA               23.60    dimethylamine

Demin water     1048.88

----------------------

Total            3077.00

Start

Finish

Grinding time

Ball mill

Transefer time